Spectral Line Shapes: Pulsed Cathodic Arc

# Text boxes

Al III spectral line broadening

Blue shift                                       Red shift

Al II spectral line broadening

Blue shift                                       Red shift

Front view:    Line is broadened considerably at all times. Line is relatively narrow at 50 s, and could possibly increase in width from 150 s on.

Side view:    Line is significantly narrower than when viewed from the front. Width does not appear to change with time.

Front view:    Line is double-peaked, and rather broad at all times. Line at 50 s is could be narrower than the others (or it could be an optical artifact due to its more pointed shape). For comparison purposes the 50 s for 2400A arc current could be shifted  to the right so that its peak is aligned with the secondary peak of the 150 s and 200 s lines

Side view:    Line is significantly narrower than when viewed from the front. Width does not appear to change with time.